## Slide 1: Diffusive interface description
sharp interface
diffuse interface
van der Walls (1894); Cahn & Hilliard (1958); Landau & Lifshitz (1955)

## Slide 2: Free energy functional
Free energy consists of two parts: local and nonlocal ( or gradient)
interface thickness
interfacial energy
energy barrier
coefficent of gradient term
0
1

## Slide 3: Variational derivative
Q1: How should the profile exactly be, in order to minimize ?
 Equilibrium
Q2: How should evolve into the equilibrium?
 Kinetics
The equilibrium is given by
.
The kinetics is also described by , depending on the field variable .

## Slide 4: Variational derivative

## Slide 5: Other advantages
There is no need for interface tracking, and topological evolution of the interfaces can be obtained by thermodynamics.
It is convenient to add new physics (e.g. mechanics, electrostatics, magnetostatics) through modification of the bulk free energy.
The phase field concept has such generality so that it can be applied to study of different microstructure resulted from different thermodynamic properties.
Thanks to the explicit formulation, phase field models are very convenient to be implemented and solved using most of the numerical methods.

## Slide 6: Bulk free energy density
Phase separation in a binary mixture

## Slide 7: Bulk free energy density
Landau free energy functional for phase transformation

## Slide 8: Bulk free energy density
Solidification

## Slide 9: Equilibrium
Equilibrium is thus the solution of the equation
for the given boundary conditions.

## Slide 10: Equilibrium
Example: Consider the bulk energy density
and the BCs at

## Slide 11: Equilibrium
Equilibrium is thus the solution of the equation
For , one has
Interface thickness
Interfacial energy

## Slide 12: Equilibrium
Free energy consists of two parts: local and nonlocal ( or gradient)
interface thickness
interfacial energy
energy barrier
coefficent of gradient term

## Slide 13: Equilibrium
Both the barrier height and the gradient coefficient effect the interface thickness and interface energy .
Instead, one also use the interface features as model parameters
Considre multiphysics problem by combining multiple phase field parameters and adding other energy contributions like elastic and electrostatic energy.

## Slide 14: Questions?